
 
Description ADSEAL AGE 510 is mono-glycidyl ether of C12-C14 fatty alcohol. The primary use of ADSEAL AGE 510 is as a reactive diluent for high viscosity epoxy resins. ADSEAL AGE 510 is compatible in all concentrations with epoxy resin and those resins blends can be cured with variety of epoxy hardeners. 
 
As with all mono-functional aliphatic reactive diluents, increase in the level of ADSEAL AGE 510 in the epoxy resin blend will increase pot life and modify cured resin properties. ADSEAL AGE 510 being aliphatic also gives advantage in terms of better non-yellowing characteristics compared to aromatic mono-functional reactive diluents. Additionally ADSEAL AGE 510 shows excellent wetting characteristics and low odour. 
 

 
Applications 	 	 
· Self leveling floorings, screeds 
· Metal and concrete primers and coatings 
· Potting and encapsulation 
· General purpose adhesives 
 

 
Specification 	 
	Appearance 	Visual 	Clear liquid 
	Colour 
	ASTM D 1544-04 
	0.5 G max. 

	Epoxy Equivalent weight 
	ASTM D 1652-04 
	275 – 300 g/eq 

	Viscosity @25ºC 
	ASTM D 2196-05 
	5 – 10 cP 

	Hydrolysable Chlorine 
	ASTM D 1726-03 
	0.1 % max. 

	Water content 
	ASTM E 203-01 
	0.1 % max. 

	Epichlorohydrin content 
	TEC-AS-P-023 
	10 ppm max. 


 

 
Typical properties * 	 
	Epoxide Value 	ASTM D 1652-04 	3.33 – 3.64 
	Density @25ºC 
	ASTM D 1475-98 
	0.9 g/ml 

	Non-volatile content 
	ASTM D 1259-06 
	100 % 

	Flash point 
	ASTM D 93 
	142°C 


 

* = Typical properties are indicated for information only 
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Packing  ADSEAL AGE 510 is packed and delivered in steel drums, 180 kg per drum as a standard pack. 
Other packs are available on request. 
 

 
Storage  	ADSEAL AGE 510 reactive diluent should be stored in original tightly closed 
container, in dry and warm conditions. Under these conditions, it has a storage life of at least two years from the date of manufacturing. 
 

 
Handling  Please refer to the MSDS of the product for more instructions on safe storage and handling of ADSEAL AGE 510. 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 

 
