
 
Description ADSEAL BGE-520 is a monofunctional reactive diluent which is the most efficient in reducing viscosity of basic epoxy resin formulations. Lower viscosity formulation allows increased filler loading and improved substrate wetting. As low level of ADSEAL BGE-520 is required to get desired viscosity, performance properties of cured resins can be maintained. 
 
	 
Salient features 	 
 
	Most efficient epoxy resin viscosity reduction  

	 
	Excellent retention of physical and thermal properties of base formulations 

	 
 
	Outstanding substrate and filler wetting characteristics 

	 
Applications 	 
 
	Adhesives 

	 
	Flooring 

	 
	Potting and encapsulations 

		 	Laminating and tooling 
 


 
Specification 	 
	Appearance 	Visual 	Clear liquid 
	Colour 
	ASTM D1544-04 (2018) 
	0.5 G max. 

	Epoxy equivalent weight 
	ASTM D1652-11 (2019) 
	145 - 155 g/eq 

	Viscosity at 25 °C 
	ASTM D2196-18Ɛ1 
	2 cPs max. 

	Hydrolysable chlorine 
	ASTM D1726-11 (2019) 
	0.1 % max. 

	Water content 
	ASTM E203-16 
	0.2 % max. 

	Epichlorohydrin content 
	TEC-AS-P-023 
	25 ppm max. 


 

 
Typical properties * 	 
	Epoxide value 	 	6.45 - 6.90 eq/kg 
	Density at 25 ºC 	 
	0.92 g/ml 

	Flash point 	 
	> 54 °C 


                                                * = Typical properties are indicated for information only 
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Packing  ADSEAL BGE-520 is packed and delivered in steel drums, 200 kg per drum as a standard pack. 
 

 
Storage  ADSEAL BGE-520 should be stored in original tightly closed container, in dry and cool conditions. Under these conditions, it has a storage life of at least two years from the date of manufacturing.  
 

 
Handling  Please refer to the SDS of the product for more instructions on safe storage and handling of ADSEAL BGE-520. 
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