
 
Description ADSEAL CGE 530is mono-functional reactive diluent based on o-Cresol. The main use of ADSEAL CGE 530is for reducing viscosity of conventional epoxy resins. The blends so prepared can be reacted with all the common curing agents employed for curing epoxy resin. 
 
ADSEAL CGE 530is known for its excellent retention of mechanical and chemical resistance properties relative to other monoepoxide diluents, also it does not influence the reactivity of the blends as it happens in the case with aliphatic monofunctional reactive diluents.  
 

 
Applications 	 	 
· Adhesives 
· Floorings and other construction applications 
· Casting 
· Tooling, potting and encapsulation 
 

 
Specification 	 
	Appearance 	Visual 	Clear liquid 
	Colour 
	ASTM D 1544-04 
	0.5 G max. 

	Epoxy Equivalent weight 
	ASTM D 1652-04 
	175 – 190 g/eq 

	Viscosity @25ºC 
	ASTM D 2196-05 
	5 – 10 cP 

	Hydrolysable Chlorine 
	ASTM D 1726-03 
	0.1 % max. 

	Water content 
	ASTM E 203-01 
	0.1 % max. 

	Epichlorohydrin content 
	TEC-AS-P-023 
	10 ppm max. 


 

 
Typical properties * 	 
	Epoxide Value 	ASTM D 1652-04 	5.26 – 5.71 
	Density @25ºC 
	ASTM D 1475-98 
	1.09 g/ml 

	Non-volatile content 
	ASTM D 1259-06 
	100 % 

	Flash point 
	ASTM D 93 
	120°C 


 

* = Typical properties are indicated for information only 
 
 
 
 

Packing  ADSEAL CGE 530is packed and delivered in steel drums, 220 kg per drum as a standard pack. 
Other packs are available on request. 
 

 
Storage  ADSEAL CGE 530reactive diluent should be stored in original tightly closed container, in dry and warm conditions. Under these conditions, it has a storage life of at least two years from the date of manufacturing. 
 

 
Handling  Please refer to the MSDS of the product for more instructions on safe storage and handling of epotec RD 105. 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
 
